| NAME | density (g/cm³) | shore A hardness (shore A) | tensile strength at break (Mpa) | elongation at break change (%) | width | thickness | Weigh Of the roll (KG) | PRICE per kg (USD/kg) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1. BLACK RUBBER DOT MAT | 1.5 | 65+5 | 2.0 4.0 | ≥250 | 1.3 m | 4.0 mm 3.0 mm | 50 kg | ? |
| 2. BLACK RUBBER WIDE RIB MAT | 1.5 | 65+5 | 2.0 4.0 | ≥250 | 1.3 m | 4.0 mm 3.0 mm | 50 kg | ? |
| 3. PLAIN RUBBER SHEET | 1.7 | 65+5 | 2.0 | ≥200 | 1.3 m 1.5 m | 1-8 mm 10-40 mm | 50 kg | ? |
| 4. INDUSTRIAL PLAIN RUBBER SHEET OIL AND PETROL RESISTANT | 1.7 | ----------- | 2.0 | ------------ | 1.2 m 1.4 m 1.5 m | 1-8 mm 10-40 mm | 50 kg | ? |