- 15C8 or SAE 1018 : STEEL 

Chemical Composition : 
% C = 0.20 Max
% Mn = 0.3 to 0.6
% S = 0.045 Max
% P = 0.035 Max
Hardness = 160 to 245 BHN.


 2) SAE 49 : Lining material

  Chemical Composition : 
% Cu = Rest
% Pb = 21 to 27
% Sn = 0.6 to 2.0
Others total = 1.0 Max
Hardness =  40 to 70 HB

Please send us the quotation at the earliest.